## Slide 1: Plasmon Hybridization in Metal Nanoparticle Clusters and Oligomers
Nicholas P. Montoni
Final Doctoral Exam
Committee Chair: Prof. David Masiello
June 5th, 2018

## Slide 2: Nanophotonics

## Slide 3: Nanophotonics
Nanotechnology
Photonics

## Slide 4: Nanophotonics
Nanotechnology
Photonics
Feynman: “there’s room at the bottom” 1954

## Slide 5: Nanophotonics
Nanotechnology
Photonics
Feynman: “there’s room at the bottom” 1954
Taniguchi: “on the basic concept of nanotechnology” 1974

## Slide 6: Nanophotonics
Nanotechnology
Photonics
Feynman: “there’s room at the bottom” 1954
Taniguchi: “on the basic concept of nanotechnology” 1974
Drexler: “molecular manufacturing” 1981

## Slide 7: Nanophotonics
Nanotechnology
Photonics
(photon electronics)
Feynman: “there’s room at the bottom” 1954
Taniguchi: “on the basic concept of nanotechnology” 1974
Drexler: “molecular manufacturing” 1981
Bell: the photophone

## Slide 8: THE PHOTOPHONE

## Slide 9: Nanophotonics
Nanotechnology
Photonics
(photon electronics)
Feynman: “there’s room at the bottom” 1954
Taniguchi: “on the basic concept of nanotechnology” 1974
Drexler: “molecular manufacturing” 1981
Bell: the photophone, 1880
Mainer: Light Amplification by Stimulated Emission of Radiation (LASER), 1960

## Slide 10: What can nanophotonics do?
Cancer therapy
Huang, X. and El-Sayed, M. A. Alexandria Journal of Medicine. 2011.

## Slide 11: What can nanophotonics do?
Chemical catalysis
N. Halas et al. Nano Lett. 2012.
S. Linic et al. ACS Nano. 2015.

## Slide 12: What can nanophotonics do?
Photovoltaic devices
Sanden, S. et al. J. Phys. Chem. C. 2015.

## Slide 13: What can nanophotonics do?
Biological sensing and imaging
Jin, Y. et al. Nat. Comm. 2010

## Slide 14: What can nanophotonics do?
Electromagnetic cloaking
Guild, M. et al. Wave Motion 2011

## Slide 15: What can nanophotonics do?
The arts!
Ruivo, A. et al. Journal of Cultural Heritage. 2008.
Duncan, K. A., et al. J. Chem. Ed. 2010.

## Slide 16: Past and present work
S. C. Quillin, C. Cherqui, N. P. Montoni, G. Li, J. P. Camden, and D. J. Masiello. “Imaging Plasmon Hybridization in Metal Nanoparticle Aggregates Using Electron Energy-Loss Spectroscopy.” J. Phys. Chem. C, 2016.
S. Griffin, N. P. Montoni, G. Li, P. J. Straney, J. E. Millstone, D. J. Masiello, and J. P. Camden. “Imaging Energy Transfer in Pt-Decorated Au Nanoprisms via Electron Energy-Loss Spectroscopy.” J. Phys. Chem. Lett., 2016.
C. Cherqui, Y. Wu, G. Li, S. C. Quillin, J. A. Busche, N. Thakkar, C. West, N. P. Montoni, P. D. Rack, J. P. Camden, and D. J. Masiello. “STEM/EELS Imaging of Magnetic Hybridization in Symmetric and Symmetry-Broken Plasmon Oligomer Dimers and All-Magnetic Fano Interference.” Nano Lett. 2016.
N. Thakkar, N. P. Montoni, C. Cherqui, and D. J. Masiello. “Quantum Plasmon Resonances in Active Environments.” Phys. Rev. B 2018.
N. P. Montoni, S. C. Quillin, C. Cherqui, and D. J. Masiello. “Magnetic Effects in Metal Nanoparticle Arrays.” ACS Photonics, Just Accepted.
N. P. Montoni, C. A. West, J. A. Busche, P. D. Rack, G. Duscher, and D. J. Masiello. “Stimulated Electron Energy-Loss Spectroscopy.” In preparation, 2018.

## Slide 17: Goals for today:
Learn about plasmons in metal nanoparticles
Learn how plasmons behave in clusters of metal nanoparticles
Qualify and quantify plasmon hybridization in mixed-metal, mixed-geometry clusters
Introduce size and magnetic effects to our model of cluster behavior
Accurately describe the plasmon resonances of large, finite clusters

## Slide 18
Metal

## Slide 19
Metal
Light

## Slide 20
Metal
Light

## Slide 21
Metal
Light

## Slide 22
Metal
Skin depth
10s of nm
Light

## Slide 23
10s of nm
(Approximately the same size as the skin depth!)
100s of nm
(one half-wavelength)
Light

## Slide 24
Eext
Light

## Slide 25
Eext
Light

## Slide 31
Electric dipole plasmon

## Slide 32
Electric dipole plasmon decay mechanisms
Light scattering

## Slide 33
Electric dipole plasmon decay mechanisms
Light scattering
Local heating

## Slide 34
Electric dipole plasmon decay mechanisms
Light scattering
Local heating
“hot electron” generation

## Slide 35: An analogy:

## Slide 36: An analogy:

## Slide 37: An analogy:

## Slide 38: An analogy:

## Slide 39: An analogy:

## Slide 40: An analogy:

## Slide 41: An analogy:

## Slide 42: An analogy:

## Slide 43: Plasmon  spring

## Slide 44: Frequency-Dependent Polarizability

## Slide 45: Time-Dependent Polarizability and Oscillator Response

## Slide 46: Time-Dependent Polarizability and Oscillator Response

## Slide 47: Time-Dependent Polarizability and Oscillator Response

## Slide 48: Time-Dependent Polarizability and Oscillator Response

## Slide 49: Time-Dependent Response of Various Metals

## Slide 50: Time-Dependent Response of Various Metals

## Slide 51: Time-Dependent Response of Various Metals

## Slide 52: Time-Dependent Response of Various Metals

## Slide 53: Time-Dependent Response of Various Metals

## Slide 54: Time-Dependent Polarizability and Oscillator Response

## Slide 55: Goals for today:
Learn about plasmons in metal nanoparticles
Learn how plasmons behave in and clusters of metal nanoparticles
Qualify and quantify plasmon hybridization in mixed-metal, mixed-geometry clusters
Introduce size and magnetic effects to our model of cluster behavior
Accurately describe the plasmon resonances of large, finite clusters

## Slide 56: Goals for today:
Learn about plasmons in metal nanoparticles
Learn how plasmons behave in clusters of metal nanoparticles
Qualify and quantify plasmon hybridization in mixed-metal, mixed-geometry clusters
Introduce size and magnetic effects to our model of cluster behavior
Accurately describe the plasmon resonances of large, finite clusters

## Slide 58
Energy
Lower-energy, anti-parallel, bonding mode
Higher-energy, parallel, anti-bonding mode

## Slide 59: Dipole-dipole interaction energy

## Slide 60: Dipole-dipole interaction energy

## Slide 61: Dipole-dipole interaction energy
Near-field Term

## Slide 62: Dipole-dipole interaction energy
Near-field Term
Intermediate-field Term

## Slide 63: Dipole-dipole interaction energy
Near-field Term
Intermediate-field Term
Far-field Term

## Slide 64: Dipole-dipole interaction energy
Near-field Term
Intermediate-field Term
Far-field Term

## Slide 65: Taking the quasistatic limit…
Quasistatic coupling is near-field coupling

## Slide 66: Quasistatic Interactions of a MNP Dimer
collinear
anti-parallel
parallel
anti-collinear

## Slide 67: Quasistatic Interactions of a MNP Dimer
collinear
anti-parallel
parallel
anti-collinear

## Slide 68: Coupled oscillator equations of motion

## Slide 69: Solving coupled oscillator equations of motion

## Slide 70: For an arbitrary number of nanoparticles:

## Slide 71: Goals for today:
Learn about plasmons in metal nanoparticles
Learn how plasmons behave in clusters of metal nanoparticles
Qualify and quantify plasmon hybridization in mixed-metal, mixed-geometry clusters
Introduce size and magnetic effects to our model of cluster behavior
Accurately describe the plasmon resonances of large, finite clusters

## Slide 72: Goals for today:
Learn about plasmons in metal nanoparticles
Learn how plasmons behave in clusters of metal nanoparticles
Qualify and quantify plasmon hybridization in mixed-metal, mixed-geometry clusters
Introduce size and magnetic effects to our model of cluster behavior
Accurately describe the plasmon resonances of large, finite clusters

## Slide 74: A Quick Intro to Electron Energy-Loss Spectroscopy (EELS)
Cherqui, C., Thakkar, N., Li, G., Camden, J. P., and Masiello, D. J. Annu. Rev. Phys. Chem. 2016.

## Slide 75: Generate a spectrum…

## Slide 76: … or generate maps!

## Slide 77: Experimental (and simulated) results

## Slide 78: Experimental (and simulated) results

## Slide 79: Experimental (and simulated) results
Split corner dipole modes!

## Slide 80: Experimental (and simulated) results

## Slide 81: A qualitative model of the nanoprism

## Slide 82: A qualitative model of the nanoprism
Energy

## Slide 83: A qualitative model of the nanoprism
This one will be relevant later…
Energy

## Slide 84: A qualitative model of the nanoprism
Energy

## Slide 85: A qualitative model of the nanoprism
Energy

## Slide 86: A qualitative model of the nanoprism
Energy

## Slide 87: Adding a (small) perturbation
Energy

## Slide 88: Adding a (small) perturbation
Energy

## Slide 89: Adding a (small) perturbation
Energy

## Slide 90: Location- and orientation- dependence of plasmon hybridization!

## Slide 91: What have we learned?
Even a small perturbation has experimentally observable impacts on the plasmonic spectrum of a nanocluster
The strength of the perturbation is location-dependent
Symmetry-breaking leads to spatial localization of energy

## Slide 92: Goals for today:
Learn about plasmons in metal nanoparticles
Learn how plasmons behave in small particles and clusters of particles
Qualify and quantify plasmon hybridization in mixed-metal, mixed-geometry clusters
Introduce size and magnetic effects to our model of cluster behavior
Accurately describe the plasmon resonances of large, finite clusters

## Slide 93: Goals for today:
Learn what a plasmon is and why we should care
Learn how plasmons behave in small particles and clusters of particles
Qualify and quantify plasmon hybridization in mixed-metal, mixed-geometry clusters
Introduce size and magnetic effects to our model of cluster behavior
Accurately describe the plasmon resonances of large, finite clusters

## Slide 94: Quasistatic coupling

## Slide 95: Fully retarded coupling
Near-field Term
Intermediate-field Term
Far-field Term

## Slide 96: Fully Retarded Interaction Energies in a MNP Dimer

## Slide 97: Fully Retarded Interaction Energies in a MNP Dimer
Quasistatic
Fully Retarded

## Slide 98: Quasistatic Solution

## Slide 99: Solutions with Retardation Effects

## Slide 100: Solutions with Retardation Effects
The same omega!

## Slide 101: Goals for today:
Learn what a plasmon is and why we should care
Learn how plasmons behave in small particles and clusters of particles
Qualify and quantify plasmon hybridization in mixed-metal, mixed-geometry clusters
Introduce size and magnetic effects to our model of cluster behavior
Accurately describe the plasmon resonances of large, finite clusters

## Slide 102: Goals for today:
Learn what a plasmon is and why we should care
Learn how plasmons behave in small particles and clusters of particles
Qualify and quantify plasmon hybridization in mixed-metal, mixed-geometry clusters
Introduce size and magnetic effects to our model of cluster behavior
Accurately describe the plasmon resonances of large, finite clusters

## Slide 104: What does “magnetic” mean?

## Slide 105: What does “magnetic” mean?

## Slide 106: Cyclic dipoles: like cyclic currents

## Slide 107: Motivation: Size Dependence
Intermediate size regime:
Greybush, J. et al. ACS Nano 2017

## Slide 108: Motivation: Accurate Model
Cherqui, C. et al. ACS Photonics 2014

## Slide 109: Motivation: Accurate Model
Quasistatic Tight-Binding Model
Energy
Cherqui, C. et al. ACS Photonics 2014

## Slide 110: Motivation: Accurate Model
Switch order!
Energy
Quasistatic Tight-Binding Model
Full-wave Simulations
Cherqui, C. et al. ACS Photonics 2014

## Slide 111: Motivation: Accurate Model
Li, C., Lee, S., Qian, Z., Woods, C., Park, S.-J., and Fakhraai, Z. J. Phys. Chem. C. 2018

## Slide 112: Model System: Arrays of Silver Nanospheres

## Slide 113: Magnetic Plasmons of the 2-mer and 3-mer

## Slide 114: Investigate spectral switching via system size

## Slide 115: The size-dependence of magnetic plasmon energetics

## Slide 116: The size-dependence of magnetic plasmon energetics

## Slide 117: Distinguishing the magnetic plasmons

## Slide 118: Directional Radiation from Electric and Magnetic Dipole Moments
x
y
z

## Slide 119: Directional Radiation from Electric and Magnetic Dipole Moments

## Slide 120: Directional Radiation from Electric and Magnetic Dipole Moments

## Slide 121: Measuring the angular dependence of scattered light
Coenen, T., Vesseur, E. J. R., and Polman, A. Appl. Phys. Lett. 2011
Coenen, T., Vesseur, E. J. R., Polman, A., and Koenderink, F. Nano Lett. 2011

## Slide 122: Angle Resolved CL spectra of magnetic oligomers

## Slide 123: Experimentally Relevant Nanoclusters
Greybush, J. et al. ACS Nano 2017

## Slide 124: Experimentally Relevant Nanoclusters

## Slide 125: Magnetic Plasmon Spectrum of Hexagonally Packed Nanoclusters

## Slide 126: Magnetic Plasmon Spectrum of Hexagonally Packed Nanoclusters

## Slide 127: Angle Resolved CL of Hexagonally Packed Nanoclusters

## Slide 128: Angle Resolved CL of Hexagonally Packed Nanoclusters

## Slide 129: Angle Resolved CL of Hexagonally Packed Nanoclusters

## Slide 130: Angle Resolved CL of Hexagonally Packed Nanoclusters

## Slide 131: What have we learned?
The spectral ordering of magnetic plasmons depends on cluster shape and size
Simulated angle-resolved CL can identify these mode-crossings

## Slide 132: Goals for today:
Learn what a plasmon is and why we should care
Learn how plasmons behave in small particles and clusters of particles
Qualify and quantify plasmon hybridization in mixed-metal, mixed-geometry clusters
Introduce size and magnetic effects to our model of cluster behavior
Accurately describe the plasmon resonances of large, finite clusters

## Slide 133: Future work: Stimulated Electron Energy-Loss Spectroscopy

## Slide 134: Future work: Stimulated Electron Energy-Loss Spectroscopy

## Slide 135: Stimulated EELS
abs

## Slide 136: Stimulated EELS

## Slide 137: Extracurriculars Community-Building and Science Advocacy
“Imagine if this type of work was a recognized part of your Ph.D.”
– Dr. Sarah Vorpahl
Founder and President, Out in STEM at UW
Founder, Chemistry Department Mentorship Network
Organizer, Strengthening STEM through Diversity
Organizer, Strategies for Cultivating Inclusion in STEM
Clean Energy Institute Education and Training Fellow
Pacific Science Center Science Communication Fellow
Speaker, 2018 March for Science - Seattle
Husky 100, 2017 Cohort
Secretary, Women in Chemical Sciences (2015-2016)

## Slide 138: Acknowledgements
My Doctoral Committee
  Prof. David Masiello
  Prof. David Ginger
  Prof. Sarah Keller
  Prof. Elizabeth Nance

## Slide 139: Acknowledgements
The Masiello group, March 2017
The Masiello Group:
  Prof. David Masiello
  Dr. Charles Cherqui
  Dr. Zhaoxia Qian
  Dr. Nicholas Bigelow
  Dr. Niket Thakkar
  Dr. Steven Quillin
  Jacob Busche
  Harrison Goldwyn
  Kevin Smith
  Elliot Beutler
  Claire West

## Slide 140: Acknowledgements
Experimental collaborators
Dr. Sarah Griffin
Prof. Jon Camden
Dr. Patrick Straney
Prof. Jill Millstone

## Slide 142: Questions?

## Slide 143
EXTRA STUFF

## Slide 145: Prism dipole moments
y-directed
x-directed

## Slide 146: Magnetic Plasmon Spectrum of Hexagonally Packed Nanoclusters

## Slide 147: Magnetic Plasmon Spectrum of Hexagonally Packed Nanoclusters

## Slide 148: The size-dependence of magnetic plasmon energetics

## Slide 149: The size-dependence of magnetic plasmon energetics

## Slide 150: How I know the quasistatic model doesn’t work at large sizes:

## Slide 151: Fully retarded model predicts multiple spectral switches

## Slide 152: Oscillations in spacing calculations are due largely to the exponential term

## Slide 153: Realistically tunable variable: interparticle distance
Urban, M. et al. JACS 2016
Tan, S. et al. Nat. Nanotech. 2011
Qian,Z. et al. JACS 2017

## Slide 154: Spacing: 2-mer
0
10

## Slide 155: Spacing: Twomer
Tiny splitting! (< .01 eV)
0
10

## Slide 156: Spacing: Twomer
0
10
0
10

## Slide 157: Spacing: Twomer
Bigger splitting! (.01 - .1 eV)
0
10

## Slide 158: Comparison of Length Scales
Length (nm)
Length (nm)

## Slide 159: Conclusions
Magnetic plasmons exhibit tunable spectral ordering
This effect is more pronounced for oligomers with larger constituent particles
0
10

## Slide 160: Characteristic Mode Wavelength
Longest Distance
Length (nm)

## Slide 161: Characteristic Mode Wavelength
Longest Distance
Retardation effects become important for this array when it is around ¼ the wavelength of light!
Length (nm)

## Slide 162: Photon-plasmon and electron-plasmon processes

## Slide 163: Photon-plasmon and electron-plasmon processes
absorption

## Slide 164: Photon-plasmon and electron-plasmon processes
absorption
scattering

## Slide 165: Photon-plasmon and electron-plasmon processes
e-
EELS

## Slide 166: Photon-plasmon and electron-plasmon processes
e-
EELS
Cathodoluminescence

## Slide 167: Photon-plasmon and electron-plasmon processes
e-
Electron energy-gain
spectroscopy

## Slide 168: Photon-plasmon and electron-plasmon processes
e-
Stimulated EELS

## Slide 169: Photon-plasmon and electron-plasmon processes
e-
Stimulated EELS

## Slide 170: Stimulated EELS