## Slide 1: Plasmon Hybridization in Clusters of Metal Nanoparticles and Magnetic Oligomers
Nicholas P. Montoni
Final Doctoral Exam
Committee Chair: Prof. David Masiello
June 5th, 2018

## Slide 2: Nanophotonics

## Slide 3: Nanophotonics
Nanotechnology
Photonics

## Slide 4: Nanophotonics
Nanotechnology
Photonics
Feynman: “there’s room at the bottom” 1954

## Slide 5: Nanophotonics
Nanotechnology
Photonics
Feynman: “there’s room at the bottom” 1954
Taniguchi: “on the basic concept of nanotechnology” 1974

## Slide 6: Nanophotonics
Nanotechnology
Photonics
Feynman: “there’s room at the bottom” 1954
Taniguchi: “on the basic concept of nanotechnology” 1974
Drexler: “molecular manufacturing” 1981

## Slide 7: Nanophotonics
Nanotechnology
Photonics
(photon electronics)
Feynman: “there’s room at the bottom” 1954
Taniguchi: “on the basic concept of nanotechnology” 1974
Drexler: “molecular manufacturing” 1981
Bell: the photophone

## Slide 8: THE PHOTOPHONE

## Slide 9: Nanophotonics
Nanotechnology
Photonics
(photon electronics)
Feynman: “there’s room at the bottom” 1954
Taniguchi: “on the basic concept of nanotechnology” 1974
Drexler: “molecular manufacturing” 1981
Bell: the photophone, 1860
Mainer: Light Amplification by Stimulated Emission of Radiation (LASER), 1960

## Slide 10: What can nanophotonics do?
Cancer therapy
Huang, X. and El-Sayed, M. A. Alexandria Journal of Medicine. 2011.

## Slide 11: What can nanophotonics do?
Chemical catalysis
N. Halas et al. Nano Lett. 2012.
S. Linic et al. ACS Nano. 2015.

## Slide 12: What can nanophotonics do?
Photovoltaic devices
Sanden, S. et al. J. Phys. Chem. C. 2015.

## Slide 13: What can nanophotonics do?
Biological sensing and imaging
Jin, Y. et al. Nat. Comm. 2010

## Slide 14: What can nanophotonics do?
Electromagnetic cloaking
Guild, M. et al. Wave Motion 2011

## Slide 15: What can nanophotonics do?
The arts!
Ruivo, A. et al. Journal of Cultural Heritage. 2008.
Duncan, K. A., et al. J. Chem. Ed. 2010.

## Slide 16: Goals for today:
Learn about plasmons in metal nanoparticles
Learn how plasmons behave in clusters of metal nanoparticles
Qualify and quantify plasmon hybridization in mixed-metal, mixed-geometry clusters
Introduce size and magnetic effects to our model of cluster behavior
Accurately describe the plasmon resonances of large, finite clusters

## Slide 17
Metal

## Slide 18
Metal
Light

## Slide 19
Metal
Light

## Slide 20
Metal
Light

## Slide 21
Metal
Skin depth
10s of nm
Light

## Slide 22
10s of nm
(Approximately the same size as the skin depth!)
100s of nm
(one half-wavelength)
Light

## Slide 23
Eext
Light

## Slide 24
Eext
Light

## Slide 30
Electric dipole plasmon

## Slide 31
Electric dipole plasmon decay mechanisms
Light scattering

## Slide 32
Electric dipole plasmon decay mechanisms
Light scattering
Local heating

## Slide 33
Electric dipole plasmon decay mechanisms
Light scattering
Local heating
“hot electron” generation

## Slide 34: An analogy:

## Slide 35: An analogy:

## Slide 36: An analogy:

## Slide 37: An analogy:

## Slide 38: An analogy:

## Slide 39: An analogy:

## Slide 40: An analogy:

## Slide 41: An analogy:

## Slide 42: The model: one particle
2

## Slide 43: Frequency-Dependent Polarizability

## Slide 44: Time-Dependent Polarizability and Oscillator Response

## Slide 45: Time-Dependent Response of Various Metals

## Slide 46: Goals for today:
Learn what a plasmon is and why we should care
Learn how plasmons behave in and clusters of metal nanoparticles
Qualify and quantify plasmon hybridization in mixed-metal, mixed-geometry clusters
Introduce size and magnetic effects to our model of cluster behavior
Accurately describe the plasmon resonances of large, finite clusters

## Slide 47: Goals for today:
Learn what a plasmon is and why we should care
Learn how plasmons behave in clusters of metal nanoparticles
Qualify and quantify plasmon hybridization in mixed-metal, mixed-geometry clusters
Introduce size and magnetic effects to our model of cluster behavior
Accurately describe the plasmon resonances of large, finite clusters

## Slide 49
Energy
Lower-energy, anti-parallel, bonding mode
Higher-energy, parallel, anti-bonding mode

## Slide 50: The model: two particles

## Slide 51: The model: two particles
2

## Slide 52: A Closer Look at the Coupling Term

## Slide 53: A Closer Look at the Coupling Term

## Slide 54: A Closer Look at the Coupling Term
Near-field Term

## Slide 55: A Closer Look at the Coupling Term
Near-field Term
Intermediate-field Term

## Slide 56: A Closer Look at the Coupling Term
Near-field Term
Intermediate-field Term
Far-field Term

## Slide 57: A Closer Look at the Coupling Term
Near-field Term
Intermediate-field Term
Far-field Term

## Slide 58: Taking the quasistatic limit…

## Slide 59: Quasistatic Interactions of a MNP Dimer

## Slide 60: Solving coupled oscillator equations of motion
2

## Slide 61: Solving coupled oscillator equations of motion

## Slide 62: For an arbitrary number of nanoparticles:

## Slide 63: Goals for today:
Learn what a plasmon is and why we should care
Learn how plasmons behave in clusters of metal nanoparticles
Qualify and quantify plasmon hybridization in mixed-metal, mixed-geometry clusters
Introduce size and magnetic effects to our model of cluster behavior
Accurately describe the plasmon resonances of large, finite clusters

## Slide 64: Goals for today:
Learn what a plasmon is and why we should care
Learn how plasmons behave in clusters of metal nanoparticles
Qualify and quantify plasmon hybridization in mixed-metal, mixed-geometry clusters
Introduce size and magnetic effects to our model of cluster behavior
Accurately describe the plasmon resonances of large, finite clusters

## Slide 65: Past and present work
S. C. Quillin, C. Cherqui, N. P. Montoni, G. Li, J. P. Camden, and D. J. Masiello. “Imaging Plasmon Hybridization in Metal Nanoparticle Aggregates Using Electron Energy-Loss Spectroscopy.” J. Phys. Chem. C, 2016.
S. Griffin, N. P. Montoni, G. Li, P. J. Straney, J. E. Millstone, D. J. Masiello, and J. P. Camden. “Imaging Energy Transfer in Pt-Decorated Au Nanoprisms via Electron Energy-Loss Spectroscopy.” J. Phys. Chem. Lett., 2016.
C. Cherqui, Y. Wu, G. Li, S. C. Quillin, J. A. Busche, N. Thakkar, C. West, N. P. Montoni, P. D. Rack, J. P. Camden, and D. J. Masiello. “STEM/EELS Imaging of Magnetic Hybridization in Symmetric and Symmetry-Broken Plasmon Oligomer Dimers and All-Magnetic Fano Interference.” Nano Lett. 2016.
N. Thakkar, N. P. Montoni, C. Cherqui, and D. J. Masiello. “Quantum Plasmon Resonances in Active Environments.” Phys. Rev. B 2018.
N. P. Montoni, S. C. Quillin, C. Cherqui, and D. J. Masiello. “Magnetic Effects in Metal Nanoparticle Arrays.” ACS Photonics, Just Accepted.
N. P. Montoni, J. A. Busche, P. D. Rack, G. Duscher, and D. J. Masiello. “Stimulated Electron Energy-Loss Spectroscopy.” In preparation, 2018.

## Slide 66: Imaging Energy Transfer in Pt-Decorated Au Nanoprisms via Electron Energy-Loss Spectroscopy
S. Griffin, N. P. Montoni, G. Li, P. J. Straney, J. E. Millstone, D. J. Masiello, and J. P. Camden. J. Phys. Chem. Lett., 2016.

## Slide 67: Catalysis – molecules adsorb

## Slide 68: Catalysis – molecules collide

## Slide 69: Catalysis – molecules react

## Slide 70: Can we enhance this process?
~ 40-50 nm
~ 150-200 nm
Like in a catalytic converter in your car!

## Slide 71: Can we enhance this process?
~ 40-50 nm
~ 150-200 nm

## Slide 72: Can we enhance this process?
~ 40-50 nm
~ 150-200 nm

## Slide 73: A Quick Intro to Electron Energy-Loss Spectroscopy (EELS)
Cherqui, C., Thakkar, N., Li, G., Camden, J. P., and Masiello, D. J. Annu. Rev. Phys. Chem. 2016.

## Slide 74: Generate a spectrum…

## Slide 75: … or generate maps!

## Slide 76: A qualitative model of the nanoprism

## Slide 77: A qualitative model of the nanoprism

## Slide 78: A qualitative model of the nanoprism
This one will be relevant later…

## Slide 79: A qualitative model of the nanoprism

## Slide 80: A qualitative model of the nanoprism

## Slide 81: A qualitative model of the nanoprism

## Slide 82: Prism dipole moments
y-directed
x-directed

## Slide 83: Adding a (small) perturbation

## Slide 84: Adding a (small) perturbation

## Slide 85: Adding a (small) perturbation

## Slide 86: Experimental (and simulated) evidence

## Slide 87: Experimental (and simulated) evidence
Split corner dipole modes!

## Slide 88: Optimizing the perturbation

## Slide 89: Are electric fields a measure of energy transfer?

## Slide 90: Are electric fields a measure of energy transfer?

## Slide 91: What have we learned?
Even a small perturbation has experimentally observable impacts on the plasmonic spectrum of a nanocluster
The strength of the perturbation is location-dependent
Changing the material of one nanoparticle changes the field enhancement around the other

## Slide 92: Goals for today:
Learn what a plasmon is and why we should care
Learn how plasmons behave in small particles and clusters of particles
Qualify and quantify plasmon hybridization in mixed-metal, mixed-geometry clusters
Introduce size and magnetic effects to our model of cluster behavior
Accurately describe the plasmon resonances of large, finite clusters

## Slide 93: Goals for today:
Learn what a plasmon is and why we should care
Learn how plasmons behave in small particles and clusters of particles
Qualify and quantify plasmon hybridization in mixed-metal, mixed-geometry clusters
Introduce size and magnetic effects to our model of cluster behavior
Accurately describe the plasmon resonances of large, finite clusters

## Slide 94: Quasistatic coupling

## Slide 95: Fully retarded coupling
Near-field Term
Intermediate-field Term
Far-field Term

## Slide 96: Fully Retarded Interaction Energies in a MNP Dimer

## Slide 97: Fully Retarded Interaction Energies in a MNP Dimer
Quasistatic
Fully Retarded

## Slide 98: Quasistatic Solution

## Slide 99: Solutions with Retardation Effects

## Slide 100: Solutions with Retardation Effects
The same omega!

## Slide 101: Goals for today:
Learn what a plasmon is and why we should care
Learn how plasmons behave in small particles and clusters of particles
Qualify and quantify plasmon hybridization in mixed-metal, mixed-geometry clusters
Introduce size and magnetic effects to our model of cluster behavior
Accurately describe the plasmon resonances of large, finite clusters

## Slide 102: Goals for today:
Learn what a plasmon is and why we should care
Learn how plasmons behave in small particles and clusters of particles
Qualify and quantify plasmon hybridization in mixed-metal, mixed-geometry clusters
Introduce size and magnetic effects to our model of cluster behavior
Accurately describe the plasmon resonances of large, finite clusters

## Slide 103: Tunable Spectral Ordering of Magnetic Plasmon Resonances in Metal Nanoparticle Clusters
Montoni N. P., Quillin, S. C., Cherqui, C., and Masiello, D. J. ACS Photonics, Just Accepted.

## Slide 104: What does “magnetic” mean?

## Slide 105: What does “magnetic” mean?

## Slide 106: Cyclic dipoles: like cyclic currents

## Slide 107: Motivation: Size Dependence
Single-oligomer regime:
Brandl, D. et al. J. Phys. Chem. B 2006.

## Slide 108: Motivation: Size Dependence
Infinite regime:
Weick, G. et al. Phys. Rev. Lett. 2013

## Slide 109: Motivation: Size Dependence
Intermediate size regime:
Greybush, J. et al. ACS Nano 2017

## Slide 110: Motivation: Accurate Model
Cherqui, C. et al. ACS Photonics 2014

## Slide 111: Motivation: Accurate Model
Quasistatic Tight-Binding Model
Energy
Cherqui, C. et al. ACS Photonics 2014

## Slide 112: Motivation: Accurate Model
Switch order!
Energy
Quasistatic Tight-Binding Model
Full-wave Simulations
Cherqui, C. et al. ACS Photonics 2014

## Slide 113: Motivation: Accurate Model
Li, C., Lee, S., Qian, Z., Woods, C., Park, S.-J., and Fakhraai, Z. J. Phys. Chem. C. 2018

## Slide 114: Model System: Arrays of Silver Nanospheres

## Slide 115: Magnetic Plasmons of the 2-mer and 3-mer

## Slide 116: Investigate spectral switching via system size

## Slide 117: The size-dependence of magnetic plasmon energetics

## Slide 118: The size-dependence of magnetic plasmon energetics

## Slide 119: The size-dependence of magnetic plasmon energetics

## Slide 120: The size-dependence of magnetic plasmon energetics

## Slide 121: Distinguishing the magnetic plasmons

## Slide 122: Directional Radiation from Electric and Magnetic Dipole Moments

## Slide 123: Directional Radiation from Electric and Magnetic Dipole Moments

## Slide 124: Directional Radiation from Electric and Magnetic Dipole Moments

## Slide 125: Directional Radiation from Electric and Magnetic Dipole Moments

## Slide 126: Directional Radiation from Electric and Magnetic Dipole Moments

## Slide 127: Directional Radiation from Electric and Magnetic Dipole Moments

## Slide 128: Measuring the angular dependence of scattered light
Coenen, T., Vesseur, E. J. R., and Polman, A. Appl. Phys. Lett. 2011
Coenen, T., Vesseur, E. J. R., Polman, A., and Koenderink, F. Nano Lett. 2011

## Slide 129: Angle Resolved CL spectra of magnetic oligomers

## Slide 130: Experimentally Relevant Nanoclusters
Greybush, J. et al. ACS Nano 2017

## Slide 131: Experimentally Relevant Nanoclusters

## Slide 132: Magnetic Plasmon Spectrum of Hexagonally Packed Nanoclusters

## Slide 133: Magnetic Plasmon Spectrum of Hexagonally Packed Nanoclusters

## Slide 134: Magnetic Plasmon Spectrum of Hexagonally Packed Nanoclusters

## Slide 135: Magnetic Plasmon Spectrum of Hexagonally Packed Nanoclusters

## Slide 136: Angle Resolved CL of Hexagonally Packed Nanoclusters

## Slide 137: Angle Resolved CL of Hexagonally Packed Nanoclusters

## Slide 138: Angle Resolved CL of Hexagonally Packed Nanoclusters

## Slide 139: Angle Resolved CL of Hexagonally Packed Nanoclusters

## Slide 140: What have we learned?
The plasmon spectrum of a cluster of metal nanoparticles depends on MNP size and cluster shape
Without retardation effects, we would never be able to describe the above phenomenon!
Angle-resolved CL is a useful tool for extracting angle-dependent radiative information about metal nanoclusters

## Slide 141: Goals for today:
Learn what a plasmon is and why we should care
Learn how plasmons behave in small particles and clusters of particles
Qualify and quantify plasmon hybridization in mixed-metal, mixed-geometry clusters
Introduce size and magnetic effects to our model of cluster behavior
Accurately describe the plasmon resonances of large, finite clusters

## Slide 142: Future work: Stimulated Electron Energy-Loss Spectroscopy

## Slide 143: Future work: Stimulated Electron Energy-Loss Spectroscopy

## Slide 144: Photon-plasmon and electron-plasmon processes

## Slide 145: Extracurriculars Community-Building and Science Advocacy
“Imagine if this type of work was a recognized part of your Ph.D.”
– Dr. Sarah Vorpahl
Founder and President, Out in STEM at UW
Founder, Chemistry Department Mentorship Network
Organizer, Strengthening STEM through Diversity
Organizer, Strategies for Cultivating Inclusion in STEM
Clean Energy Institute Education and Training Fellow
Pacific Science Center Science Communication Fellow
Speaker, 2018 March for Science - Seattle
Husky 100, 2017 Cohort
Secretary, Women in Chemical Sciences (2015-2016)
Hillel UW Nachshon Award (2018)

## Slide 146: Acknowledgements
The Masiello group, March 2017
The Masiello Group:
  Prof. David Masiello
  Dr. Charles Cherqui
  Dr. Zhaoxia Qian
  Dr. Nicholas Bigelow
  Dr. Niket Thakkar
  Dr. Steven Quillin
  Jacob Busche
  Harrison Goldwyn
  Kevin Smith
  Elliot Beutler
  Claire West

## Slide 147: Acknowledgements
My Doctoral Committee
  Prof. David Ginger
  Prof. Sarah Keller
  Prof. Elizabeth Nance

## Slide 148: Acknowledgements

## Slide 149: Questions?

## Slide 150
EXTRA STUFF

## Slide 151: Time-Dependent Response of Various Metals

## Slide 152: Time-Dependent Response of Various Metals

## Slide 153: Time-Dependent Response of Various Metals

## Slide 154: Time-Dependent Response of Various Metals

## Slide 156: How I know the quasistatic model doesn’t work at large sizes:

## Slide 157: Fully retarded model predicts multiple spectral switches

## Slide 158: Oscillations in spacing calculations are due largely to the exponential term

## Slide 159: Realistically tunable variable: interparticle distance
Urban, M. et al. JACS 2016
Tan, S. et al. Nat. Nanotech. 2011
Qian,Z. et al. JACS 2017

## Slide 160: Spacing: 2-mer
0
10

## Slide 161: Spacing: Twomer
Tiny splitting! (< .01 eV)
0
10

## Slide 162: Spacing: Twomer
0
10
0
10

## Slide 163: Spacing: Twomer
Bigger splitting! (.01 - .1 eV)
0
10

## Slide 164: Comparison of Length Scales
Length (nm)
Length (nm)

## Slide 165: Conclusions
Magnetic plasmons exhibit tunable spectral ordering
This effect is more pronounced for oligomers with larger constituent particles
0
10

## Slide 166: Characteristic Mode Wavelength
Longest Distance
Length (nm)

## Slide 167: Characteristic Mode Wavelength
Longest Distance
Retardation effects become important for this array when it is around ¼ the wavelength of light!
Length (nm)