## Slide 1: Plasmon Hybridization in Clusters of Metal Nanoparticles and Magnetic Oligomers
Nicholas P. Montoni
Final Doctoral Exam
Committee Chair: Prof. David Masiello
June 5th, 2018

## Slide 2: Nanophotonics

## Slide 3: Nanophotonics
Nanotechnology
Photonics

## Slide 4: Nanophotonics
Nanotechnology
Photonics
Feynman: “there’s room at the bottom” 1954

## Slide 5: Nanophotonics
Nanotechnology
Photonics
Feynman: “there’s room at the bottom” 1954
Taniguchi: “on the basic concept of nanotechnology” 1974

## Slide 6: Nanophotonics
Nanotechnology
Photonics
Feynman: “there’s room at the bottom” 1954
Taniguchi: “on the basic concept of nanotechnology” 1974
Drexler: “molecular manufacturing” 1981

## Slide 7: Nanophotonics
Nanotechnology
Photonics
(photon electronics)
Feynman: “there’s room at the bottom” 1954
Taniguchi: “on the basic concept of nanotechnology” 1974
Drexler: “molecular manufacturing” 1981
Bell: the photophone

## Slide 8: THE PHOTOPHONE

## Slide 9: Nanophotonics
Nanotechnology
Photonics
(photon electronics)
Feynman: “there’s room at the bottom” 1954
Taniguchi: “on the basic concept of nanotechnology” 1974
Drexler: “molecular manufacturing” 1981
Bell: the photophone, 1860
Mainer: Light Amplification by Stimulated Emission of Radiation (LASER), 1960

## Slide 10: What can nanophotonics do?
Cancer therapy
Huang, X. and El-Sayed, M. A. Alexandria Journal of Medicine. 2011.

## Slide 11: What can nanophotonics do?
Chemical catalysis
N. Halas et al. Nano Lett. 2012.
S. Linic et al. ACS Nano. 2015.

## Slide 12: What can nanophotonics do?
Photovoltaic devices
Sanden, S. et al. J. Phys. Chem. C. 2015.

## Slide 13: What can nanophotonics do?
Biological sensing and imaging
Jin, Y. et al. Nat. Comm. 2010

## Slide 14: What can nanophotonics do?
Electromagnetic cloaking
Guild, M. et al. Wave Motion 2011

## Slide 15: What can nanophotonics do?
The arts!
Ruivo, A. et al. Journal of Cultural Heritage. 2008.
Duncan, K. A., et al. J. Chem. Ed. 2010.

## Slide 16: Goals for today:
Learn about plasmons in metal nanoparticles
Learn how plasmons behave in clusters of metal nanoparticles
Qualify and quantify plasmon hybridization in mixed-metal, mixed-geometry clusters
Introduce size and magnetic effects to our model of cluster behavior
Accurately describe the plasmon resonances of large, finite clusters

## Slide 17
Metal

## Slide 18
Metal
Light

## Slide 19
Metal
Light

## Slide 20
Metal
Light

## Slide 21
Metal
Skin depth
10s of nm
Light

## Slide 22
10s of nm
(Approximately the same size as the skin depth!)
100s of nm
(one half-wavelength)
Light

## Slide 23
Eext
Light

## Slide 24
Eext
Light

## Slide 30
Electric dipole plasmon

## Slide 31: An analogy:

## Slide 32: An analogy:

## Slide 33: An analogy:

## Slide 34: An analogy:

## Slide 35: An analogy:

## Slide 36: An analogy:

## Slide 37: An analogy:

## Slide 38: An analogy:

## Slide 39: The model: one particle
2

## Slide 40: Frequency-Dependent Polarizability

## Slide 41: Time-Dependent Polarizability and Oscillator Response

## Slide 42: Time-Dependent Response of Various Metals

## Slide 43: Goals for today:
Learn what a plasmon is and why we should care
Learn how plasmons behave in and clusters of metal nanoparticles
Qualify and quantify plasmon hybridization in mixed-metal, mixed-geometry clusters
Introduce size and magnetic effects to our model of cluster behavior
Accurately describe the plasmon resonances of large, finite clusters

## Slide 44: Goals for today:
Learn what a plasmon is and why we should care
Learn how plasmons behave in clusters of metal nanoparticles
Qualify and quantify plasmon hybridization in mixed-metal, mixed-geometry clusters
Introduce size and magnetic effects to our model of cluster behavior
Accurately describe the plasmon resonances of large, finite clusters

## Slide 46
Energy
Lower-energy, anti-parallel, bonding mode
Higher-energy, parallel, anti-bonding mode

## Slide 47: The model: two particles

## Slide 48: The model: two particles
2

## Slide 49: A Closer Look at the Coupling Term

## Slide 50: A Closer Look at the Coupling Term

## Slide 51: A Closer Look at the Coupling Term
Near-field Term

## Slide 52: A Closer Look at the Coupling Term
Near-field Term
Intermediate-field Term

## Slide 53: A Closer Look at the Coupling Term
Near-field Term
Intermediate-field Term
Far-field Term

## Slide 54: A Closer Look at the Coupling Term
Near-field Term
Intermediate-field Term
Far-field Term

## Slide 55: Taking the quasistatic limit…

## Slide 56: Quasistatic Interactions of a MNP Dimer

## Slide 57: Solving coupled oscillator equations of motion
2

## Slide 58: Solving coupled oscillator equations of motion

## Slide 59: For an arbitrary number of nanoparticles:

## Slide 60: Goals for today:
Learn what a plasmon is and why we should care
Learn how plasmons behave in clusters of metal nanoparticles
Qualify and quantify plasmon hybridization in mixed-metal, mixed-geometry clusters
Introduce size and magnetic effects to our model of cluster behavior
Accurately describe the plasmon resonances of large, finite clusters

## Slide 61: Goals for today:
Learn what a plasmon is and why we should care
Learn how plasmons behave in clusters of metal nanoparticles
Qualify and quantify plasmon hybridization in mixed-metal, mixed-geometry clusters
Introduce size and magnetic effects to our model of cluster behavior
Accurately describe the plasmon resonances of large, finite clusters

## Slide 62: Past and present work
S. C. Quillin, C. Cherqui, N. P. Montoni, G. Li, J. P. Camden, and D. J. Masiello. “Imaging Plasmon Hybridization in Metal Nanoparticle Aggregates Using Electron Energy-Loss Spectroscopy.” J. Phys. Chem. C, 2016.
S. Griffin, N. P. Montoni, G. Li, P. J. Straney, J. E. Millstone, D. J. Masiello, and J. P. Camden. “Imaging Energy Transfer in Pt-Decorated Au Nanoprisms via Electron Energy-Loss Spectroscopy.” J. Phys. Chem. Lett., 2016.
C. Cherqui, Y. Wu, G. Li, S. C. Quillin, J. A. Busche, N. Thakkar, C. West, N. P. Montoni, P. D. Rack, J. P. Camden, and D. J. Masiello. “STEM/EELS Imaging of Magnetic Hybridization in Symmetric and Symmetry-Broken Plasmon Oligomer Dimers and All-Magnetic Fano Interference.” Nano Lett. 2016.
N. Thakkar, N. P. Montoni, C. Cherqui, and D. J. Masiello. “Quantum Plasmon Resonances in Active Environments.” Phys. Rev. B 2018.
N. P. Montoni, S. C. Quillin, C. Cherqui, and D. J. Masiello. “Magnetic Effects in Metal Nanoparticle Arrays.” ACS Photonics, Just Accepted.
N. P. Montoni, J. A. Busche, P. D. Rack, G. Duscher, and D. J. Masiello. “Stimulated Electron Energy-Loss Spectroscopy.” In preparation, 2018.

## Slide 63: Imaging Energy Transfer in Pt-Decorated Au Nanoprisms via Electron Energy-Loss Spectroscopy
S. Griffin, N. P. Montoni, G. Li, P. J. Straney, J. E. Millstone, D. J. Masiello, and J. P. Camden. J. Phys. Chem. Lett., 2016.

## Slide 64: Catalysis – molecules adsorb

## Slide 65: Catalysis – molecules collide

## Slide 66: Catalysis – molecules react

## Slide 67: Can we enhance this process?
~ 40-50 nm
~ 150-200 nm
Like in a catalytic converter in your car!

## Slide 68: Can we enhance this process?
~ 40-50 nm
~ 150-200 nm

## Slide 69: Can we enhance this process?
~ 40-50 nm
~ 150-200 nm

## Slide 70: A Quick Intro to Electron Energy-Loss Spectroscopy (EELS)
Cherqui, C., Thakkar, N., Li, G., Camden, J. P., and Masiello, D. J. Annu. Rev. Phys. Chem. 2016.

## Slide 71: Generate a spectrum…

## Slide 72: … or generate maps!

## Slide 73: A qualitative model of the nanoprism

## Slide 74: A qualitative model of the nanoprism

## Slide 75: A qualitative model of the nanoprism
This one will be relevant later…

## Slide 76: A qualitative model of the nanoprism

## Slide 77: A qualitative model of the nanoprism

## Slide 78: A qualitative model of the nanoprism

## Slide 79: Prism dipole moments
y-directed
x-directed

## Slide 80: Adding a (small) perturbation

## Slide 81: Adding a (small) perturbation

## Slide 82: Adding a (small) perturbation

## Slide 83: Experimental (and simulated) evidence

## Slide 84: Experimental (and simulated) evidence
Split corner dipole modes!

## Slide 85: Optimizing the perturbation

## Slide 86: Are electric fields a measure of energy transfer?

## Slide 87: Are electric fields a measure of energy transfer?

## Slide 88: What have we learned?
Even a small perturbation has experimentally observable impacts on the plasmonic spectrum of a nanocluster
The strength of the perturbation is location-dependent
Changing the material of one nanoparticle changes the field enhancement around the other

## Slide 89: Goals for today:
Learn what a plasmon is and why we should care
Learn how plasmons behave in small particles and clusters of particles
Qualify and quantify plasmon hybridization in mixed-metal, mixed-geometry clusters
Introduce size and magnetic effects to our model of cluster behavior
Accurately describe the plasmon resonances of large, finite clusters

## Slide 90: Goals for today:
Learn what a plasmon is and why we should care
Learn how plasmons behave in small particles and clusters of particles
Qualify and quantify plasmon hybridization in mixed-metal, mixed-geometry clusters
Introduce size and magnetic effects to our model of cluster behavior
Accurately describe the plasmon resonances of large, finite clusters

## Slide 91: Quasistatic coupling

## Slide 92: Fully retarded coupling
Near-field Term
Intermediate-field Term
Far-field Term

## Slide 93: Fully Retarded Interaction Energies in a MNP Dimer

## Slide 94: Fully Retarded Interaction Energies in a MNP Dimer
Quasistatic
Fully Retarded

## Slide 95: Quasistatic Solution

## Slide 96: Solutions with Retardation Effects

## Slide 97: Solutions with Retardation Effects
The same omega!

## Slide 98: Goals for today:
Learn what a plasmon is and why we should care
Learn how plasmons behave in small particles and clusters of particles
Qualify and quantify plasmon hybridization in mixed-metal, mixed-geometry clusters
Introduce size and magnetic effects to our model of cluster behavior
Accurately describe the plasmon resonances of large, finite clusters

## Slide 99: Goals for today:
Learn what a plasmon is and why we should care
Learn how plasmons behave in small particles and clusters of particles
Qualify and quantify plasmon hybridization in mixed-metal, mixed-geometry clusters
Introduce size and magnetic effects to our model of cluster behavior
Accurately describe the plasmon resonances of large, finite clusters

## Slide 100: Tunable Spectral Ordering of Magnetic Plasmon Resonances in Metal Nanoparticle Clusters
Montoni N. P., Quillin, S. C., Cherqui, C., and Masiello, D. J. ACS Photonics, Just Accepted.

## Slide 101: What does “magnetic” mean?

## Slide 102: What does “magnetic” mean?

## Slide 103: Cyclic dipoles: like cyclic currents

## Slide 104: Motivation: Size Dependence
Single-oligomer regime:
Brandl, D. et al. J. Phys. Chem. B 2006.

## Slide 105: Motivation: Size Dependence
Infinite regime:
Weick, G. et al. Phys. Rev. Lett. 2013

## Slide 106: Motivation: Size Dependence
Intermediate size regime:
Greybush, J. et al. ACS Nano 2017

## Slide 107: Motivation: Accurate Model
Cherqui, C. et al. ACS Photonics 2014

## Slide 108: Motivation: Accurate Model
Quasistatic Tight-Binding Model
Energy
Cherqui, C. et al. ACS Photonics 2014

## Slide 109: Motivation: Accurate Model
Switch order!
Energy
Quasistatic Tight-Binding Model
Full-wave Simulations
Cherqui, C. et al. ACS Photonics 2014

## Slide 110: Motivation: Accurate Model
Li, C., Lee, S., Qian, Z., Woods, C., Park, S.-J., and Fakhraai, Z. J. Phys. Chem. C. 2018

## Slide 111: Model System: Arrays of Silver Nanospheres

## Slide 112: Magnetic Plasmons of the 2-mer and 3-mer

## Slide 113: Investigate spectral switching via system size

## Slide 114: The size-dependence of magnetic plasmon energetics

## Slide 115: The size-dependence of magnetic plasmon energetics

## Slide 116: The size-dependence of magnetic plasmon energetics

## Slide 117: The size-dependence of magnetic plasmon energetics

## Slide 118: Distinguishing the magnetic plasmons

## Slide 119: Directional Radiation from Electric and Magnetic Dipole Moments

## Slide 120: Directional Radiation from Electric and Magnetic Dipole Moments

## Slide 121: Directional Radiation from Electric and Magnetic Dipole Moments

## Slide 122: Directional Radiation from Electric and Magnetic Dipole Moments

## Slide 123: Directional Radiation from Electric and Magnetic Dipole Moments

## Slide 124: Directional Radiation from Electric and Magnetic Dipole Moments

## Slide 125: Measuring the angular dependence of scattered light
Coenen, T., Vesseur, E. J. R., and Polman, A. Appl. Phys. Lett. 2011
Coenen, T., Vesseur, E. J. R., Polman, A., and Koenderink, F. Nano Lett. 2011

## Slide 126: Angle Resolved CL spectra of magnetic oligomers

## Slide 127: Experimentally Relevant Nanoclusters
Greybush, J. et al. ACS Nano 2017

## Slide 128: Experimentally Relevant Nanoclusters

## Slide 129: Magnetic Plasmon Spectrum of Hexagonally Packed Nanoclusters

## Slide 130: Magnetic Plasmon Spectrum of Hexagonally Packed Nanoclusters

## Slide 131: Magnetic Plasmon Spectrum of Hexagonally Packed Nanoclusters

## Slide 132: Magnetic Plasmon Spectrum of Hexagonally Packed Nanoclusters

## Slide 133: Angle Resolved CL of Hexagonally Packed Nanoclusters

## Slide 134: Angle Resolved CL of Hexagonally Packed Nanoclusters

## Slide 135: Angle Resolved CL of Hexagonally Packed Nanoclusters

## Slide 136: Angle Resolved CL of Hexagonally Packed Nanoclusters

## Slide 137: What have we learned?
The plasmon spectrum of a cluster of metal nanoparticles depends on MNP size and cluster shape
Without retardation effects, we would never be able to describe the above phenomenon!
Angle-resolved CL is a useful tool for extracting angle-dependent radiative information about metal nanoclusters

## Slide 138: Goals for today:
Learn what a plasmon is and why we should care
Learn how plasmons behave in small particles and clusters of particles
Qualify and quantify plasmon hybridization in mixed-metal, mixed-geometry clusters
Introduce size and magnetic effects to our model of cluster behavior
Accurately describe the plasmon resonances of large, finite clusters

## Slide 139: Future work: Stimulated Electron Energy-Loss Spectroscopy

## Slide 140: Future work: Stimulated Electron Energy-Loss Spectroscopy

## Slide 141: Photon-plasmon and electron-plasmon processes

## Slide 142: Extracurriculars Community-Building and Science Advocacy
“Imagine if this type of work was a recognized part of your Ph.D.”
– Dr. Sarah Vorpahl
Founder and President, Out in STEM at UW
Founder, Chemistry Department Mentorship Network
Organizer, Strengthening STEM through Diversity
Organizer, Strategies for Cultivating Inclusion in STEM
Clean Energy Institute Education and Training Fellow
Pacific Science Center Science Communication Fellow
Speaker, 2018 March for Science - Seattle
Husky 100, 2017 Cohort
Secretary, Women in Chemical Sciences (2015-2016)
Hillel UW Nachshon Award (2018)

## Slide 143: Acknowledgements
The Masiello group, March 2017
The Masiello Group:
  Prof. David Masiello
  Dr. Charles Cherqui
  Dr. Zhaoxia Qian
  Dr. Nicholas Bigelow
  Dr. Niket Thakkar
  Dr. Steven Quillin
  Jacob Busche
  Harrison Goldwyn
  Kevin Smith
  Elliot Beutler
  Claire West

## Slide 144: Acknowledgements
My Doctoral Committee
  Prof. David Ginger
  Prof. Sarah Keller
  Prof. Elizabeth Nance

## Slide 145: Acknowledgements

## Slide 146: Questions?

## Slide 147
EXTRA STUFF

## Slide 148: Time-Dependent Response of Various Metals

## Slide 149: Time-Dependent Response of Various Metals

## Slide 150: Time-Dependent Response of Various Metals

## Slide 151: Time-Dependent Response of Various Metals

## Slide 153: How I know the quasistatic model doesn’t work at large sizes:

## Slide 154: Fully retarded model predicts multiple spectral switches

## Slide 155: Oscillations in spacing calculations are due largely to the exponential term

## Slide 156: Realistically tunable variable: interparticle distance
Urban, M. et al. JACS 2016
Tan, S. et al. Nat. Nanotech. 2011
Qian,Z. et al. JACS 2017

## Slide 157: Spacing: 2-mer
0
10

## Slide 158: Spacing: Twomer
Tiny splitting! (< .01 eV)
0
10

## Slide 159: Spacing: Twomer
0
10
0
10

## Slide 160: Spacing: Twomer
Bigger splitting! (.01 - .1 eV)
0
10

## Slide 161: Comparison of Length Scales
Length (nm)
Length (nm)

## Slide 162: Conclusions
Magnetic plasmons exhibit tunable spectral ordering
This effect is more pronounced for oligomers with larger constituent particles
0
10

## Slide 163: Characteristic Mode Wavelength
Longest Distance
Length (nm)

## Slide 164: Characteristic Mode Wavelength
Longest Distance
Retardation effects become important for this array when it is around ¼ the wavelength of light!
Length (nm)